## Slide 1
Generator RIGOL DG4102
Oscilloscope RIGOL DS1104
Measurement cell
PCB designed to accommodate wire samples of varying lengths
Bridge scheme
Channel 2
Channel 1
Signal

## Slide 2

Vout
R0
R2
R1
R3
Rw
V0

## Slide 3
Vout
R0
R1
R3
Rw
VM


R0
R1
R3
Rw
V0
The output signal (blue) observed at the balanced bridge when Rw is substituted with a ferromagnetic microwire of the same DC resistance.
Vw

## Slide 4
Vout
R0
R1
R3
Rw
VM

The output signal (blue) observed at the balanced bridge when Rw is substituted with a ferromagnetic microwire of the same DC resistance.

## Slide 5
a
l

## Slide 6

R0
R1
R3
Rw

## Slide 7
All measured voltages must be saved in Volts (V)
Resistors in the bridge circuit are measured in Ohms ()
Microwire radius a and length l are measured in meters (m)
(A/m)
(T)
microwire
DC resistance

## Slide 8
Copy and paste the directory with the experimental data, e.g. E:\Dropbox\MISiS\BH-loop\Experimental data
Type the file name, e.g. 50kHz
Type the time increment in the scientific format, e.g. 5e-8
Your scale coefficients here (1 by default)
Used to smooth the BH curves (5 by default)
GUI in Python: run main.py
Change the file name and run the code. All output files will be rewritten.
Stop the code

## Slide 9
Structure of the CSV file: no header, two columns, comma delimiter
First column: signal response
Second column: excitation sinusoid (more than two periods)